华樾精细化工（昆山）有限公司

TECHNICAL DATA SHEET

PRODUCT NAME:DISPERSANT

TYPE:1996

| PROPERTIES | DATA | STANDARD REGULATION |
| --- | --- | --- |
| 外观APPEARANCE | 黄色透明液体Yellow transparent liquid | Q/YQEH73 standard |
| PH值PH VALUE | 7-8 |  |
| 粘度VISCOSITY | 50±5 KU |  |
| 非挥发物质Non-volatile matter (10 min., 150 °C | 30% |  |

| *MEASURED BY ELECTRON MICROSCOPE |  |  |  |  |
| --- | --- | --- | --- | --- |

RECOMMEND APPLICATION:

INDUSTRIAL PAINTS,PIGMENT INK, PESTICIDES,COSMETICS etc.

PACKING: 25/200 KG/TANK

ADD：江苏昆山花桥立德企业园5-1

www.hy-chemical.cn